|  |
| --- |
| **CHEMSIZE BF-100**  **ONE SHOT SIZING AGENT**  *A UNIQUE BLEND OF HIGHLY HYDROLYSED POLYMER*  *& FORTIFIED WITH SAPONIFIED FAT* . |

**ACTS AS CATALYST TO MODIFY THE MAIZE STARCH BY HYDROLYSING IT DURING SIZE COOKING & IMPARTS A MAGICAL CHANGE IN CHARACTERISTICS OF SIZE LIQUOR & MADE IT SUBSTANTIVE TOWARDS YARN LIKE POLY / COTTON, COTTON / VISCOSE & COTTON / CELLUOSIC FIBRES BASED BLENDED YARN.**

|  |
| --- |
| *PHYSICAL PROPERTIES* |

**APPEARANCE**  : Opaque Thick Jell like Pasty Consistency.

**CHEMICAL NATURE** : Highly Basic Anionic in Nature.

**COMPATIBILITY** : Only Compatible with Nonionic & Anionic Ingredients.

*APPLICATION*

Sometimes it is desirable to size the yarn without PVA & WAXY Substances. The sizing recipe having rich PVA is very difficult to be removed during desizing prior to dyeing & bleaching process.

Thanks to special formulation of ***CHEMSIZE BF-100*** it almost eliminates such elements / products to be the part of size liquor. Only one product is enough to have routine characteristics of the size liquor. This minimizes not only the cost but also maximizes the weaving efficiency of the looms of either type like AIR JET / SULZER etc.

In routine practice & results obtained by applying the product ***CHEMSIZE BF-100*** , it has been preferred & consumed due to its extraordinary sizing & excellent performance at almost 50% less cost than sizing with PVA & TALLOW like ingredients.

***CHEMSIZE BF-100*** is very simple to apply. Just add water, desired quantity of Maize Starch & a

little quantity of ***CHEMSIZE BF-100*** ***.*** No third additive like PVA or Acrylic is required. Routine cooking is carried out & then the size is ready to apply on Slasher Sizing Machine.

It has been observed on sizing machine that there is least dusting as compared to normal sizing recipe having even rich PVA or other binders . On looms , as no fluff or beads formation is produced , therefore looms run without any stoppage . Better efficiency has been recorded as compared to routine / normal sizing.

***CHEMSIZE BF-100*** is equally suitable for the cotton & cotton polyester blended yarn. Even poly / viscose blended yarn can be sized with little change in recipe. It is suitable for all counts prior to bulk production & by following the recipe as mentioned below.

“Cont’d on next sheet

**ORGANO CHEMICALS ( PVT ) LTD*.***

**2ND FLOOR, ZIA COMMERCIAL PLAZA ,P-135,STREET # 10 WAKILAN,**

**KATCHERY BAZAR, FAISALABAD,PAKISTAN.**

**PH: 92-41-2624946 FAX: 92-41-2636504 E.MAIL:organo@fsd.comsats.net.pk**

***GENERAL RECIPE***

***FOR COTTON & COTTON / POLYESTER BLEND FABRICS OF LOW TO MEDIUM COVER FACTOR.***

MAIZE STARCH (non modified) = 75-80 KG

WATER = 800 LITRE

***CHEMSIZE BF-100***  ***= 03 KG***

WAX = 02 KG

Cooking is completed within 35 – 40 minutes. If there is FOAM, then add a little ANTIFOAM to avoid any foam problem during sizing.

***FOR FABRICS HAVING HIGH COVER FACTOR / FINE COUNT 40 OR ABOVE..***

MAIZE STARCH (non modified) = 80 KG

WATER = 800 LITRE

***CHEMSIZE BF-100***  ***= 03 KG***

WAX = 02 KG

***FOR THE YARN LIKE PV., PP. BEFORE RUNNING, SMALL TRIAL SHOULD BE CARRIED OUT TO TUNE UP THE RECIPE. HOWEVER FOLLOWING RECIPE MAY BE FOLLOWED FOR TRIAL.***

MAIZE STARCH( non modified) = 75-80 KG

WATER = 800 LITRE

***CHEMSIZE BF-100***  ***= 03 KG***

PVA = 4-5 KG

WAX = 01 KG

***PRECAUTIONS***

No adverse effect of the product has been observed. However as the product is highly basic in nature , therefore it is advisable to follow the precautionary measurements during handling & storage . For detailed precautions, follow the product MSDS.

***RECOMMENDATIONS***

The size film is non sticky to Slasher Drying Cylinders / Drums. However Teflon Coated Drying Cylinders / Drums are preferred for trouble free sizing.

***ADVANTAGES***

* **VERY SIMPLE TO APPLY.**
* **NO DUSTING OR FLUFF DURING SIZING OR ON LOOM.**
* **LEAST BREAKAGE & HIGH WEAVING EFFECIENCY.**
* **VERY ECONOMICAL. ALMOST 40 – 50 % LESS COST.**
* **DESIZING REQUIRES NO SPECIAL TREATMENT.**
* **SMOOTH & SOFT FABRIC CONSTRUCTION.**

***PACKING / STORAGE***

**\*** In 200 KG net Steel drums / 150 KG net PVC Drums.

**\*** Store under shade & cool place. Avoid storage in direct sunlight or in hot climatic conditions.

*The information in this document is based on our present knowledge and must not be considered as a guarantee of specific properties.*

*-----------------------------------------------------------------------------------------------------------------------------------------------------------------*

**ORGANO CHEMICALS ( PVT ) LTD*.***

**2ND FLOOR, ZIA COMMERCIAL PLAZA ,P-135,STREET # 10 WAKILAN,**

**KATCHERY BAZAR, FAISALABAD,PAKISTAN.**

**PH: 92-41-2624946 FAX: 92-41-2636504 E.MAIL:organo@fsd.comsats.net.pk**

**MATERIAL SAFETY DATA SHEET**

|  |
| --- |
| ***SECTION - 1 : MATERIAL IDENTIFICATION & USE*** |

**MATERIAL NAME IDENTIFIER** : ***CHEMSIZE BF-100*** **----** *ONE SHOT SIZING AGENT.*

**MANUFACTURER / SUPPLIER** : ***ORGANO CHEMICALS (PVT) LTD.,***

2nd. FLOOR, ZIA COMMERCIAL PLAZA, STREET 10 WAKILAN

KATCHERY BAZAR, FAISALABAD , PAKISTAN.

**CHEMICAL NAME** : A UNIQUE BLEND OF HIGHLY HYDROLYSED VINYL POLYMER &

FORTIFIED WITH SAPONIFIED FAT.

|  |
| --- |
| ***SECTION - 2 : HAZARDOUS INGREDIENTS*** |

**HAZARDOUS INGREDIENTS**  : NON HAZARDOUS INGREDIENTS

|  |
| --- |
| ***SECTION – 3 : PHYSICAL DATA*** |

**PHYSICAL STATE :** WHITE THICK GELL LIKE PASTY CONSISTANCY.

|  |
| --- |
| *SECTION – 4 : FIRE & EXPLOSIVE DATA.* |

**FLAMMABILITY :** NON FLAMEABLE

|  |
| --- |
| ***SECTION - 5 : REACTIVITY DATA*** |

**CHEMICAL STABILITY :** BELOW 30o C, STORE UNDER SHADE IN COOL PLACE.

**COMPATABILITY :** ONLY COMPATIBLE WITH NONIONIC & ANIONICS INGREDIENTS.

|  |
| --- |
| ***SECTION – 6 : TOXICOLOGICAL PROPERTIES*** |

**ROUTE OF ENTRY :** SKIN CONTACT - HARMLESS

EYE CONTACT - CAUSE IRRITATION

**EFFECT OF CHRONIC**  **:** LD 5O MATERIAL - NOT AVAILABLE

**EXPOSURE TO MATERIAL** IRRITANCY OF MATERIAL - IRRITATE TO EYES

|  |
| --- |
| ***SECTION – 7 : PREVENTIVE MEASURES*** |

**PERSONAL PROTECTIVE**  :EYE ( SPECIFY ) - WEAR GOGGLES

###### EQUIPMENT : FOOT WEAR (SPECIFY) - WEAR RUBBER BOOTS

###### :CLOTHING (SPECIFY) - LONG SLEEVE COVERALL

**ENGINEERING CONTROLS** (SPECIFY :NOT NECESSARY

E.G VENTILATION ENCLOSED PROCESS)

**LEAK & SPILL PROCEEDURE** : SPILLAGE CAUSES SLIPPERY. COLLECT INTO A CLOSED CONTAINER.

WASH OUT THE AREA WITH PLENTY OF WATER.

**WASTE DISPOSAL** : INCINERATE OR TREAT A SEWEAGE PLANT.

**HANDLING PROCEEDURE** : WASH HANDS & FACE DAILY AFTER WORK OR WHEN CONTAMINATED.

**STORAGE REQUIREMENTS** : STORE BELOW 30 C & AVOID DIRECT SUNLIGHT.

: DO NOT LEAVE OPEN TO THE ATMOSPHERE.

: STORE AT A FIXED PLACE. KEEP THE CONTAINERS WELL TIGHT

AFTER USE

: DO NOT USE EMPTY DRUMS OR CONTAINERS FOR OTHER PURPOSE

& KEEP AT A FIXED PLACE UNTIL DISPOSING OFF PROPERLY.

|  |
| --- |
| ***SECTION - 8 : FIRST AID MEASURES*** |

**SKIN CONTACT** : IMMEDIATELY REMOVE THE CONTAMINATED CLOTHING.

WASH THE SKIN THOROUGHLY WITH WATER & SOAP.

**EYE CONTACT** : IMMEDIATELY WASH THE EYES WITH PLENTY OF WATER

FOR MORE THAN 15 MINUTES.

**INHALATION** : STEP INTO AREA OF FRESH AIR & LIE QUIET.

**SWALLOWING** : DRINK WATER & INDUCE VOMITTING. TAKE 50 gr. OF

ACTIVATED CHARCOAL BY MOUTH.

**SPECIAL ADVICE**  : ***SEEK MEDICAL ATTENTION AFTER THE ABOVE***

***MEASURES IF NECESSARY.***

**SOURCES USED** : MANUFACTURER’S INTERNAL MANUALS.